Lab Session for Organic Photovoltaics (OPVs) Device Fabrication

- Cleaning procedure for patterned ITO glass substrates:

- Sonication for 15 min in detergent water.

- Sonication for 15 min in DI water.

- Sonication for 15 min in absolute ethyl alcohol.

- Drying using air gun and then storing at 60 oC in furnace for 1 hour before using.

- Solution preparation using CF as solvent. The following solutions will be prepared:

- D18:Y6 (1:1.2) (without additive).

- D18:Y6 (1:1.2) (with additive).

- D18 only.

- UV-Ozone treatment for 20 min for substrates.

- PEDOT:PSS deposition on cleaned substrates @ 4000 rmp. PEDOT:PSS is a hole transporting layer (HTL).

- After that, samples transferred inside the glove box for active layer deposition. The following conditions will be followed:

- D18:Y6 (1:1.2) (without additive) @ 3000 rpm.

- D18:Y6 (1:1.2) (with additive) @ 3000 rpm.

- D18 only @ 3000 rpm.

- Further thermal annealing for active layers.

- Spin-coat the electron transport layer PDINN @ 3000 rpm.

- Masking of the samples for top electrode deposition using shadow mask.

- Loading the samples in the thermal evaporator for 100 nm Ag deposition.

- Unloading the devices after electrode deposition.

- Device performance measurement using solar simulator.